Welding Procedure Specification 
Recommended Addendum

WPS __NASA-A572-SMAW_Rev 1____________________

Client ____Sample_______________________________

Welding document owner ___NASA__________________________

Project: ____Sample Review____

Date of review ___10/8/2025____

Client has final deposition responsibility to determine which if any of the recommended addenda recommendations are required.  Client may copy recommendations

WPS ___ NASA-A572-SMAW_Rev 1__________

Addendum __ SAMPLE 2025-10-8__

The instructions contained in this addendum are in addition to those provided in the WPS proper.  All instructions in this addendum are to be followed and take presidents over any in WPS proper.  This addendum is to be attached to the WPS for all purposes (fabrication, inspection, inclusion in data book, etc.).  Use of the reviewed WPS constitutes acceptance of this addendum.    In lieu of this addendum a revised or new WPS may be proposed.

Welding is limited for A572 grade 50 P#1 Cr#1

Joints limited to single vee and single bevel.  Double groove, U, and J welds shown in Attachment one are not allowed

Retainers are not allowed

Base material thickness allowed is limited to 1.625” max thickness (pending PQR correction/addenda)

SMAW deposit maximum thickness is increased to maximum base metal thickness allowed by WPS

Welds are to be performed in the flat position

Initial cleaning to be by brushing or welding.  Wet metal to be dried by heating

Backing is allowed for fillet welds only